## Slide 1
Three-dimensional Zn/LiFePO4 aqueous hybrid-ion battery for renewable energy integration into electrical grids.
Toru Hara 1,2,3,* Anton Antonov 1, Nurzhan Umirov 1,
Zhumabay Bakenov 1,2,3
1* Institute of Batteries LLC, Kabanbay Batyr Ave. 53, Astana, Kazakhstan, hara.toru@nu.edu.kz
2 Nazarbayev University Research and Innovation System, Kabanbay Batyr Ave. 53, Astana, Kazakhstan
3 Nazarbayev University, Kabanbay Batyr Ave. 53, Astana, Kazakhstan
56th Battery Conference Japan, Nagoya, Japan, 11-13th, November, 2015

## Slide 2
Three-dimensional Zn anode
The merits are,
8-sec anode preparation -> 2.8 mAh/cm2,
Balanced anode/cathode capacity ratio,
Hopefully, short circuit failure suppression.

## Slide 3
Introduction
Renewable energy integration into electrical grids is crucial for energy security, leading to the highly secured communication network, traffic control, industrial activities, etc.
Renewable energies are intermittent and cannot be easily directly integrated to electric grids without using batteries.
These batteries must be safe and inexpensive from the viewpoint of life-cycle cost.
Aqueous batteries are non-flammable that can be a great merit compared with traditional lithium-ion batteries that use flammable organic electrolyte solutions.

## Slide 4
Lead-acid battery:
toxic, life-cycle cost is not low
NiMH battery:
Gigacell costs $2500 kWh-1 25 years-1
There are some new technologies that are currently under the field test.
Conventional aqueous battery
Pb, PbO2, H2SO4

## Slide 5
Zn/LiFePO4 system is a promising candidate.
No toxic materials.
Zn anode that delivers a higher gravimetric capacity (Zn, 818 mAh g-1) than metal hydride (e.g., LaNi3.55Co0.75Mn0.4Al0.3, 300 mAh/g or less) and a comparable potential (-0.76 V vs. Standard Hydrogen Electrode, SHE) in aqueous media with metal hydride (e.g., LaNi3.55Co0.75Mn0.4Al0.3, -0.75 to -0.85 V vs. SHE).
Comparable cost with lead-acid battery when using Zn foil.
Previous Work
[N. Yesibolati, N. Umirov, A. Koishybay, M. Omarova, I. Kurmanbayeva, Y. Zhang, Y. Zhao, Z. Bakenov, Electrochimica Acta 152 (2015) 505-511.]

## Slide 6
The problem is zinc dendrite formation resulting in internal short circuit failure and how to balance anode/cathode capacities.
Challenging issue
Facilitating long-range electronic conductivity through the inner core of zinc electrode,
Amplification of electrified interfaces to distribute current uniformly throughout the electrode structure,
Forming partially confined void volume elements within the interior of the porous zinc anode that expedite dissolution/deposition.
In short, POROUS, MONOLITHIC, THREE-DIMENSIONAL, and APERIODIC ARCHITECTURE.
Counter measure
[J. F. Parker, C. N. Chervin, E. S. Nelson, D. R. Rolison, J. W. Long, Energy Environ. Sci. 7 (2014) 1117-1124; J. F. Parker, E. S. Nelson, M. D. Wattendorf, C. N. Chervin, J. W. Long, D. R. Rolison, ACS Appl. Mater. Interfaces 6 (2014) 19471–19476.]

## Slide 7
Parker’s counter measure
Sintered Zn
Our counter measure
Electrodeposited Zn
onto CFP
Porous
Monolithic
Three-dimensional aperiodic
Counter measure

## Slide 8
Present work
Onto the current collector, carbon fiber paper (CFP), zinc was cathodically electroplated.
CFP
Zn @ CFP

## Slide 9
Present work
Constant current density of 500 mA cm-2.
Deposition time of 8 sec.
Zn 3.4 mg cm-2, 2.8 mAh cm-2
Electrolyte solution:
0.52 mol L-1 ZnSO4·7H2O,
0.15 mol L-1 (NH4)2SO4,
0.7 g L-1 polyacrylamide (PAA, MW=200,000),
0.05 g L-1 thiourea,
40 g L-1 H3BO3 (pH = 4)
2/98 vol.% ethanol/water with 0.1 g L-1 sodium dodecyl sulfate (SDS) (ethanol and SDS were added as wetting agents).
0.13-mm-thick graphite backing-plate is attached to a CFP beforehand by using carbon paint adhesive [PELCO® high temperature carbon paste (silicate)].

## Slide 10
[TGP-H-060 (190-μm-thick) or TGP-H-120 (370-μm-thick), Toray Industry Inc.]
Carbon fiber felt (cheap)
Future plan
Cost reduction

## Slide 11
Thank you 