## Slide 1
THESIS DEFENSE
The Combined Effect of Waste Glass Sand and Glass Fiber on the Improvement of Thermal Property of Aerated Concrete
Inzhu Yerbolat, ID 201460756
Civil and Environmental Engineering Department

## Slide 2
Background and Introduction
Thesis Structure
Experimental Program
Test Result Analysis
Thermal Conductivity Prediction Model
Energy Saving Effect of NAAC
Feasbility of NAAC
8. Conclusion
Civil and Environmental Engineering Department
OUTLINE

## Slide 3
1. BACKGROUND AND INTRODUCTION
Civil and Environmental Engineering Department

## Slide 4
Civil and Environmental Engineering Department
1.BACKGROUND
Lightweight
Energy-efficient
Excellent thermal insulative
Fire resistance
Reduction of supporting loads
Economy in construction of foundation/reinforcement
Reduction of energy consumption
Reduction of operation payment for heating/cooling
Aerated Concrete
Types | 
Autoclaved Aerated Concrete | None-autoclaved Aerated Concrete
Curing under some pressure | Normal curing
Risk on environment and economy | No risk

## Slide 5
Civil and Environmental Engineering Department
1.INTRODUCTION
Research Problem
Waste Glass Accumulation
World: 200 million tons/yr
KZ: 340 thousand tons/yr
8.8% - recycled
91.2% - disposed
Energy Consumption
Research Goal
Prepare Aerated Concrete, using waste glasses as aggregate
Evaluate their effect on the improvement of the thermal property
Research Hypothesis
Synergetic effect
Glass sand replacement decreases the thermal conductivity
Glass fiber replacement improves the mechanical property

## Slide 6
2. THESIS STRUCTURE
Civil and Environmental Engineering Department

## Slide 7
1. Literature Review
2. Experimental Program
3. Test Result Analysis
5. Evaluation of Energy Saving Effect of NAAC material: Design Builder Software
4. Modelling an Equation for Prediction of Thermal Conductivity: Minitab Software
Non-Autoclaved Aerated Concrete
Effect of Glass Sand and Glass Fiber
2.2 Material Preparation and its Characterization
2.1 Optimization of Mixture Proportion
Sieve Analysis – ASTM C136
Chemical Composition – ASTM C114
Aggregate Properties – ASTM C556, C127, C128
2.3 Non-Autoclaved Aerated Concrete Preparation and Properties Testing
Thermal Conductivity
Compressive Strength – ASTM C39
Flexural Strength – ASTM C78
Ultrasonic Pulse Velocity – ASTM C597
Alkali-Silica Reaction – ASTM C1567
Porosity, Specific Gravity, Density – ASTM C830
Parameters
Normal Sand
Waste Glass Sand
Glass Fiber
Cement/Fly ash
Water to Cementous Ratio
6. Documentation: Thesis, Research paper, Presentation
2. THESIS STRUCTURE

## Slide 8
3. EXPERIMENTAL PROGRAM
Civil and Environmental Engineering Department

## Slide 9
3.EXPERIMENTAL PROGRAM – MIX DESIGN
No | Cement | Fly ash | Normal Sand | Waste Glass Sand | Waste Glass Fiber
M1 | 100 | 0 | 100 | 0 | 0
M2 | 100 | 0 | 85 | 15 | 0
M3 | 100 | 0 | 70 | 30 | 0
M4 | 85 | 15 | 70 | 30 | 0
M5 | 70 | 30 | 70 | 30 | 0
M6 | 100 | 0 | 70 | 30 | 1% of N. sand by volume
M7 | 100 | 0 | 70 | 30 | 2% of N. sand by volume
M8 | 100 | 0 | 70 | 30 | 3% of N. sand by volume
M9 | 70 | 30 | 70 | 30 | 1% of N. sand by volume
M10 | 70 | 30 | 70 | 30 | 2% of N. sand by volume
M11 | 70 | 30 | 70 | 30 | 3% of N. sand by volume
Table 2. Mixture Parameters
Series
Series 1: M1-M3, glass sand replacement
Series 2: M3-M5, fly ash replacement
Series 3: M6-M8, combination of glass sand and glass fiber
Series 4: M9-M11, combination of glass sand, glass fiber and fly ash.

## Slide 10
Civil and Environmental Engineering Department
3. EXPERIMENTAL PROGRAM
Properties | # of Samples | Test Methods | Testing Date | Equipment
Thermal Conductivity | 12 | ASTM E1530 | 7/14/28 | ИТС-1 “150”
Compressive Strength + UPV | 12 + 3 | ASTM C39 | 7/14/28 | Compression Testing Machine
Flexural Strength | 12 | ASTM C78 | 7/14/28 | Compression Testing Machine
Porosity, Density, Absorption | Same samples | ASTM C830 | 7/14/28 | Weighing machine
# of samples for each batch = 39
Total # of samples = 11 batches * 39 samples = 396
Table 3. Testing Properties

## Slide 11
4. TEST RESULTS ANALYSIS
Civil and Environmental Engineering Department

## Slide 12
Figure 4.1.
(a) Thermal conductivity of NAAC containing glass sand
b) Thermal conductivity of NAAC containing fly ash.
(c) Thermal conductivity of NAAC containing glass fiber
(d) Thermal conductivity of NAAC containing glass fiber with fly ash.
(a)
(b)
(c)
(d)
4. TEST RESULTS: Thermal conductivity and mixture parameters
Chart: Mixtures
| M1 (0% GS) | M2 (15% GS) | M3 (30% GS)
7 day | 0.22493 | 0.13247 | 0.13078
14 day | 0.2104 | 0.11467 | 0.12505
28 day | 0.2263 | 0.1362 | 0.1403
Chart: Mixtures
| M3 (0% GF) | M4 (15% FA) | M5 (30% FA)
7 day | 0.13078 | 0.13743 | 0.13233
14 day | 0.12505 | 0.17103 | 0.21273
28 day | 0.1403 | 0.21665 | 0.2213
Chart: Mixtures
| M9 (1% GF + 30% FA) | M10 (2% GF + 30% FA) | M11 (3% GF+30 % FA)
7 day | 0.15873 | 0.15863 | 0.1861
14 day | 0.1364 | 0.17397 | 0.17685
28 day | 0.11817 | 0.18603 | 0.1764
Chart: Mixtures
| M6 (1% GF) | M7 (2% GF) | M8 (3% GF)
7 day | 0.15957 | 0.18607 | 0.167
14 day | 0.18017 | 0.18725 | 0.19683
28 day | 0.22023 | 0.1436 | 0.19993

## Slide 13
Figure 4.2. Relationship between thermal conductivity and density (a) 7-day cured (b) 14-day cured (c) 28-day cured (d) 28-day cured except M1
(a)
(b)
(c)
(d)
4. TEST RESULTS: Thermal conductivity and density
Chart: Density
| 1.5780000000000001 | 1.377 | 1.3080000000000001 | 1.4139999999999999 | 1.4330000000000001 | 1.4219999999999999 | 1.4450000000000001 | 1.4590000000000001 | 1.355 | 1.377 | 1.4119999999999999
7-day cured | 0.2249 | 0.1325 | 0.1308 | 0.1374 | 0.1323 | 0.1596 | 0.1861 | 0.167 | 0.1587 | 0.1586 | 0.1861
Chart: Density
| 1.5780000000000001 | 1.25 | 1.3 | 1.4 | 1.41 | 1.37 | 1.44 | 1.43 | 1.33 | 1.41 | 1.41
 | 0.2104 | 0.1147 | 0.1251 | 0.171 | 0.2127 | 0.1802 | 0.1873 | 0.1968 | 0.1364 | 0.174 | 0.1769
Chart: Density
| 0.9 | 1.28 | 1.34 | 1.46 | 1.5 | 1.51 | 1.5 | 1.55 | 1.4 | 1.45 | 1.45
 | 0.2263 | 0.1362 | 0.1403 | 0.2167 | 0.2213 | 0.2202 | 0.1436 | 0.1999 | 0.1182 | 0.186 | 0.1764
Chart: Density
| 1.28 | 1.34 | 1.46 | 1.5 | 1.51 | 1.5 | 1.55 | 1.4 | 1.45 | 1.45
 | 0.1362 | 0.1403 | 0.2167 | 0.2213 | 0.2202 | 0.1436 | 0.1999 | 0.1182 | 0.186 | 0.1764
Table 4.1 Relationship between thermal conductivity and density |  |  | 
 | 7 day | 14 day | 28 day
Overall | 58,47% | 74,56 | 0,53
Overall (except mixture 1) | 21,72% | 82,71% | 46,06%
Series 1 | 94,68 | 99,82 | 97,26
Series 2 | 31,94 | 83,84 | 96,36
Series 3 | 16,15 | 54,6 | 19,32
Series 4 | 85,13 | 99,59 | 98,29

## Slide 14
Figure 4.3. Relationship between thermal conductivity and porosity of 7-day cured samples (a) overall (b) by series
(a)
(b)
4. TEST RESULTS: Thermal conductivity and porosity
Chart: Porosity
| 45.832999999999998 | 70.650999999999996 | 62.609000000000002 | 57.753999999999998 | 66.736000000000004 | 55.912999999999997 | 52.997 | 53.173999999999999 | 58.82 | 57.784999999999997 | 55.231000000000002
 | 0.2249 | 0.1325 | 0.1308 | 0.1374 | 0.1323 | 0.1596 | 0.1861 | 0.167 | 0.1587 | 0.1586 | 0.1861
Chart: Porosity
| 45.832999999999998 | 70.650999999999996 | 62.609000000000002
Series 1 | 0.2249 | 0.1325 | 0.1325 | 0.1325 | 0.1308 | 0.1308 | 0.1308
Series 2 | 0.1308 | 0.1374 | 0.1323 | 0.1323
Series 3 | 0.1596 | 0.1861 | 0.167
Series 4 | 0.1587 | 0.1586 | 0.1861
Table 4.2 Relationship between thermal conductivity and porosity |  |  | 
 | 7 day | 14 day | 28 day
Overall | 76,74% | 57,93 | 14,92
Series 1 | 89,92 | 97,3 | 96,11
Series 2 | 58,96 | 79,14 | 5,39
Series 3 | 56,62 | 67,48 | 57,82
Series 4 | 91,98 | 75,87 | 97,28

## Slide 15
Figure 4.4. Relationship between thermal conductivity and absorption of 14-day cured samples (a) overall (b) by series
(a)
(b)
4. TEST RESULTS: Thermal conductivity and absorption
Chart: Absorption
| 41.31 | 94.73 | 88.5 | 65.099999999999994 | 64.400000000000006 | 69.69 | 60.97 | 62.51 | 82.63 | 69.150000000000006 | 75.02
 | 0.2104 | 0.1147 | 0.1251 | 0.171 | 0.2127 | 0.1802 | 0.1873 | 0.1968 | 0.1364 | 0.174 | 0.1769
Chart: Absorption
| 41.31 | 94.73 | 94.73 | 94.73 | 88.5
Series 1 | 0.2104 | 0.1147 | 0.1251
Series 2 | 0.1251 | 0.171 | 0.2127
Series 3 | 0.1802 | 0.1873 | 0.1968
Series 4 | 0.1364 | 0.174 | 0.1769
Table 4.3. Relationship between thermal conductivity and absorption |  |  | 
 | 7 day | 14 day | 28 day
Overall | 75,75% | 81,55 | 62,5
Series 1 | 95,04 | 99,02 | 97,65
Series 2 | 81,91 | 76,49 | 46,64
Series 3 | 100 | 51,23 | 47,08
Series 4 | 86,42 | 75,87 | 98,14

## Slide 16
Figure 4.5. The effect of curing age on thermal conductivity (a) Series 1 (b) Series 2 (c) Series 3 (d) Series 4
(a)
(b)
(c)
(d)
4. TEST RESULTS: Thermal conductivity and curing age
Chart: Curing age, days
| 7 | 14 | 28
M1 | 0.2249 | 0.2104 | 0.2263
M2 | 0.1325 | 0.1147 | 0.1362
M3 | 0.1308 | 0.1251 | 0.1403
Chart: Curing age, days
| 7 | 14 | 28
M3 | 0.1308 | 0.1251 | 0.1403
M4 | 0.1374 | 0.171 | 0.2167
M5 | 0.1323 | 0.2127 | 0.2213
Chart: Curing age, days
| 7 | 14 | 28
M6 | 0.1596 | 0.1802 | 0.2202
M7 | 0.1861 | 0.1873 | 0.1436
M8 | 0.167 | 0.1968 | 0.1999
Chart: Curing age, days
| 7 | 14 | 28
M9 | 0.1587 | 0.1364 | 0.1182
M10 | 0.1586 | 0.174 | 0.186
M11 | 0.1861 | 0.1769 | 0.1764

## Slide 17
Figure 4.6.
(a) The compressive strength of NAAC containing glass sand
b) The compressive strength of NAAC containing fly ash
(c) The compressive strength of NAAC containing glass fiber
(d) The compressive strength of NAAC containing combined glass sand, glass fiber and fly ash
(a)
(b)
(c)
(d)
4. TEST RESULTS: Compressive Strength Development
Chart: Compressive Strength (MPa)
| M1 (0% GS) | M2 (15% GS) | M3 (30% GS)
7 day | 0.434 | 0.747 | 0.919
14 day | 0.311 | 0.843 | 1.083
28 day | 0.403 | 0.891 | 1.26
Chart: Compressive Strength (MPa)
| M3 (0% FA) | M4 (15% FA) | M5 (30% FA)
7 day | 0.919 | 1.295 | 0.798
14 day | 1.083 | 1.695 | 0.945
28 day | 1.26 | 1.766 | 1.702
Chart: Compressive Strength (MPa)
| M3 (no GF) | M6 (1% GF) | M7 (2% GF) | M8 (3% GF)
7 day | 0.919 | 1.851 | 2.35 | 3.892
14 day | 1.083 | 1.96 | 2.069 | 4.074
28 day | 1.26 | 2.258 | 2.71 | 5.189
Chart: Compressive Strength (MPa)
| M9 (1% GF) | M10 (2% GF) | M11 (3% GF)
7 day | 1.708 | 1.914 | 1.94
14 day | 2.359 | 2.259 | 1.84
28 day | 1.768 | 3.496 | 3.498

## Slide 18
4. TEST RESULTS: Compressive Strength an UPV
Chart: UPV, m/s
| 1037.3333333333333 | 1287.75 | 1453.5 | 1659.25 | 1388 | 1817 | 1915 | 2225 | 1769.5 | 1889.75 | 1752.5
7-day | 0.434 | 0.747 | 0.919 | 1.295 | 0.798 | 1.851 | 2.35 | 3.892 | 1.708 | 1.914 | 1.94
Table 4.4 Relationship between the compressive strength and UPV |  |  | 
 | 7-day | 14-day | 28-day
Overall | 87,83 | 87,06 | 90,26
Series 1 | 99,76 | 99,71 | 95,88
Series 2 | 100 | 95,95 | 61,08
Series 3 | 100 | 52,62 | 100
Series 4 | 91,5 | 91,74 | 98,8
Figure 4.8. The relationship between compressive strength and UPV.

## Slide 19
Figure 4.7.
(a) The flexural strength of NAAC containing glass sand
b) The flexural strength of NAAC containing fly ash
(c) The flexural strength of NAAC containing glass fiber
(d) The flexural strength of NAAC containing combined glass sand, glass fiber and fly ash
(a)
(b)
(c)
(d)
4. TEST RESULTS: Flexural Strength Development
Chart: Flexxural Strength (MPa)
| M1 (0% GS) | M2 (15% GS) | M3 (30% GS)
7 day | 0.642 | 1.865 | 1.778
14 day | 1.047 | 0.816 | 1.903
28 day | 1 | 1.894 | 1.643
Chart: Flexxural Strength (MPa)
| M3 (0% FA) | M4 (15% FA) | M5 (30% FA)
7 day | 1.778 | 1.444 | 1.937
14 day | 1.903 | 1.394 | 1.943
28 day | 1.643 | 1.611 | 0.563
Chart: Flexxural Strength (MPa)
| M6 (1% GF) | M7 (2% GF) | M8 (3% GF)
7 day | 1.496 | 1.618 | 2.156
14 day | 1.593 | 1.469 | 1.502
28 day | 1.531 | 1.615 | 2.152
Chart: Flexxural Strength (MPa)
| M9 (1% GF) | M10 (2% GF) | M11 (3% GF)
7 day | 0.694 | 1.476 | 1.492
14 day | 2.006 | 1.735 | 1.88
28 day | 1.919 | 1.801 | 1.883

## Slide 20
Figure 4.8 The relationship between (a) density and porosity (b) density and absorption (c) absorption and porosity
5. TEST RESULTS: Physical Properties
Chart: Porosity
| 45.832999999999998 | 59.96 | 61.08 | 54.75 | 54.59 | 56.22 | 54.17 | 54.72 | 60.15 | 57.68 | 60.19
 | 1.578 | 1.25 | 1.3 | 1.4 | 1.4 | 1.4 | 1.41 | 1.37 | 1.44 | 1.43 | 1.33 | 1.41 | 1.41
Table 4.5 Relationship between porosity and density |  |  | 
 | 7 day | 14 day | 28 day
 | R2 |  | 
Overall | 46,24% | 63,36 | 10,09
Series 1 | 70,73 | 95,74 | 99,99
Series 2 | 0,9 | 99,63 | 17,1
Series 3 | 81,99 | 98,26 | 84,19
Series 4 | 98,82 | 81,14 | 99,88
Chart: Absorption
| 41.31 | 94.73 | 88.5 | 65.099999999999994 | 64.400000000000006 | 69.69 | 60.97 | 62.51 | 82.63 | 69.150000000000006 | 75.02
 | 1.578 | 1.25 | 1.3 | 1.4 | 1.4 | 1.4 | 1.41 | 1.37 | 1.44 | 1.43 | 1.33 | 1.41 | 1.41
Table 4.6. Relationship between density and absorption |  |  | 
 | 7 day | 14 day | 28 day
Overall | 58,07% | 69,52 | 32,89
Series 1 | 80,5 | 99,88 | 90,09
Series 2 | 27,61 | 99,68 | 28,2
Series 3 | 86,44 | 99,89 | 91,2
Series 4 | 99,97 | 81,14 | 100
Chart: Porosity
| 45.832999999999998 | 59.96 | 61.08 | 54.75 | 54.59 | 56.22 | 54.17 | 54.72 | 60.15 | 57.68 | 60.19
 | 41.31 | 94.73 | 88.5 | 65.1 | 64.4 | 69.69 | 60.97 | 62.51 | 82.63 | 69.15 | 75.02
Table 4.7 Relationship between porosity and absorption |  |  | 
 | 7 day | 14 day | 28 day
Overall | 96,17% | 86,34 | 18,45
Series 1 | 98,7 | 97,04 | 88,08
Series 2 | 63,57 | 100 | 30,46
Series 3 | 99,63 | 97,26 | 98,84
Series 4 | 99,19 | 100 | 99,92

## Slide 21
5. THERMAL CONDUCTIVITY PREDICTION MODEL
Civil and Environmental Engineering Department

## Slide 22
5. Thermal Conductivity Prediction Model
Multivariate Linear Regression Analysis
MINITAB Statistical Software
Table 5.1. Simulation Analysis of 14-day cured sample results |  |  |  |  |  |  |  |  |  |  |  | 
# | R2 | Cp | S | Abs | ρ | P | x | NS | C | FA | GS | GF
1 | 86.2 | 4.5 | 0.012215 |  |  | x |  | x | x |  | x | x
2 | 85 | 4.8 | 0.012748 | x | x | x | x | x |  |  |  | 
3 | 84.1 | 6.2 | 0.013126 |  |  | x | x | x | x |  | x | x
4 | 83.7 | 6.3 | 0.13286 | x | x | x | x | x |  |  | x | x
5 | 85.8 | 7.1 | 0.012393 | x | x | x | x | x | x |  | x | x
6 | 79.7 | 8.1 | 0.014826 | x |  | x | x | x | x | x | x | x
7 | 80.1 | 9.0 | 0.014688 | x | x | x | x | x | x | x | x | x
Criteria:
R2 – exactness coefficients – higher is better
Cp – set of terms, closer to the number of variables
S – standard error, lower is better.

## Slide 23
5. Thermal Conductivity Prediction Model
– 0,000263 Cement + 0,0731 GS + 0,0771 GF
where, λ – thermal conductivity, Abs – absorption, ρ – density, P – porosity, Δ x – thickness, NS – normal sand, GS – glass sand, GF – glass fiber
Table 5.2. MLR analyses of NAAC samples |  |  | 
 | 7-day | 14-day | 28-day
Best-fit model | 2,54 + 0,0053 Δx + 0,158 ρ - 0,0053 P + 0,0014 Abs - 0,0251 NS + 0,000015 Cement - 0,0259 GS - 0,0204 GF |  | -6,7 - 0,003331 Abs + 0,246 ρ+ 0,00170 P + 0,00203 Δx+ 0,068 NS - 0,000970 Cement + 0,065 GS + 0,046 GF
R2 | 70.8 % | 85.8% | 80.5%
S | 0.015742 | 0.012393 | 0.017615
Table 5.2. MLR analyses of NAAC samples |  |  | 
 | 7-day | 14-day | 28-day
Best-fit model | 2,54 + 0,0053 Δx + 0,158 ρ - 0,0053 P + 0,0014 Abs - 0,0251 NS + 0,000015 Cement - 0,0259 GS - 0,0204 GF |  | -6,7 - 0,003331 Abs + 0,246 ρ+ 0,00170 P + 0,00203 Δx+ 0,068 NS - 0,000970 Cement + 0,065 GS + 0,046 GF
R2 | 70.8 % | 85.8% | 80.5%
S | 0.015742 | 0.012393 | 0.017615
(eq. 1)

## Slide 24
6. ENERGY SAVING SIMULATION
Civil and Environmental Engineering Department

## Slide 25
6.Evaluation of Energy Conservation
Figure 6.1. 5-storey residential building model for energy simulation
Floor: 5
1 floor area: 770,88 m2
Total area: 3854,4 m2
Table 6.1 Properties of wall structure materials |  |  |  |  |  | 
Materials | Thickness (mm) | Thermal conductivity (W/m·K) |  | Specific heat (J/kg·K) | Density (kg/m3) | Cost
Decorative Plaster | 10 | 0.33 |  | 2040 | 520 | 1.26 (GBP/m2)
Mineral Wool | 100 | 0.038 |  | 840 | 140 | 33.56 (GBP/m3)
NAAC | 300 | From Experimental Results |  |  |  | 25.61 (GBP/m3)
Cement/Plaster/Mortar | 15 | 0.72 | 840 |  | 1760 | 0.75 (GBP/m2)

## Slide 26
6. Design Builder Simulation Results
Figure 6.2 Heating Load of NAAC
Chart: Heating Load (kWh)
| Jan | Feb | Mar | Apr | May | Jun | Jul | Aug | Sept | Oct | Nov | Dec
M1 | 78404.22 | 64687.91 | 50151.53 | 14501.02 | 22.94 | 0 | 0 | 0 | 652.48 | 18030.69 | 51827.87 | 70078.04
M2 | 76391.86 | 62894.61 | 48531.57 | 13712.29 | 15.24 | 0 | 0 | 0 | 705.73 | 17619.88 | 50658.02 | 68147.18
M3 | 76689.46 | 63152 | 48758.35 | 13802.03 | 15.9 | 0 | 0 | 0 | 717.21 | 17727.75 | 50862.37 | 68429.31
M4 | 77737.48 | 64054.95 | 49539.3 | 14103.59 | 18.23 | 0 | 0 | 0 | 767.32 | 18134.11 | 51605.88 | 69409.13
M5 | 78431.29 | 64633.12 | 50042.72 | 14288.63 | 19.78 | 0 | 0 | 0 | 807.03 | 18418.84 | 52133.37 | 70046.64
M6 | 77908.47 | 64198.77 | 49659.4 | 14143.78 | 18.54 | 0 | 0 | 0 | 781.23 | 18214.7 | 51743.55 | 69564.96
M7 | 78030.02 | 64307.43 | 49757.45 | 14189.71 | 18.94 | 0 | 0 | 0 | 779.43 | 18244.38 | 51815.2 | 69682.31
M10 | 77793.74 | 64103.34 | 49580.88 | 14120.66 | 18.37 | 0 | 0 | 0 | 769.39 | 18154.67 | 51648.62 | 69461.77
M11 | 77847.95 | 64149.46 | 49620.42 | 14135.09 | 18.48 | 0 | 0 | 0 | 772.54 | 18177 | 51688.61 | 69511.86
Temperature (°C) | -10.59 | -10.17 | -5.49 | 5.81 | 14.21 | 18.4 | 20.02 | 17.63 | 12.12 | 5.44 | -3.89 | -7.67
Chart: Cooling Load (kWh)
| Jan | Feb | Mar | Apr | May | Jun | Jul | Aug | Sept | Oct | Nov | Dec
M1 | 0 | 0 | 1.68 | 222.96 | 1568.06 | 6611.89 | 10519.73 | 5653.06 | 346.24 | 0 | 0 | 0
M2 | 0 | 0 | 0.8 | 170.62 | 1365.82 | 6322.98 | 10411.98 | 5606.38 | 327.75 | 0 | 0 | 0
M3 | 0 | 0 | 1.11 | 199.43 | 1457.82 | 6482.11 | 10435.13 | 5530.32 | 317.26 | 0 | 0 | 0
M4 | 0 | 0 | 1.21 | 203.27 | 1477.84 | 6504.01 | 10454.03 | 5561.68 | 323.62 | 0 | 0 | 0
M5 | 0 | 0 | 1.81 | 227.97 | 1590.17 | 6638.08 | 10535.12 | 5672.43 | 351.14 | 0 | 0 | 0
M6 | 0 | 0 | 1.3 | 206.86 | 1493.94 | 6523.54 | 10465.7 | 5577.29 | 327.26 | 0 | 0 | 0
M7 | 0 | 0 | 1.32 | 207.8 | 1498.08 | 6528.62 | 10468.55 | 5580.89 | 328.12 | 0 | 0 | 0
M8 | 0 | 0 | 1.57 | 218.6 | 1548.01 | 6587.88 | 10504.71 | 5632.82 | 341.36 | 0 | 0 | 0
M9 | 0 | 0 | 1.17 | 201.72 | 1469.79 | 6495.26 | 10446.75 | 5549.42 | 321.12 | 0 | 0 | 0
M10 | 0 | 0 | 1.27 | 206.63 | 1490.86 | 6521.78 | 10460.05 | 5566.38 | 325.26 | 0 | 0 | 0
M11 | 0 | 0 | 1.28 | 206.22 | 1490.87 | 6520.05 | 10463.06 | 5573.4 | 326.38 | 0 | 0 | 0
Temperature | -10.59 | -10.17 | -5.49 | 5.81 | 14.21 | 18.4 | 20.02 | 17.63 | 12.12 | 5.44 | -3.89 | -7.67
Figure 6.3 Cooling Load of NAAC
Table 6.2 Temperature Data |  |  |  |  |  |  |  |  |  |  | 
Temperature (°C) |  |  |  |  |  |  |  |  |  |  | 
Jan. | Feb. | March | Apr. | May | June | July | Aug. | Sept. | Oct. | Nov. | Dec.
-10,6 | -10,2 | -5,5 | 5,8 | 14,2 | 18,4 | 20,0 | 17,6 | 12,1 | 5,4 | -3,9 | -7,7

## Slide 27
6. Design Builder Simulation Results
Table 6.3 Site and Source Energy Results of NAAC |  |  |  | 
Mixt. | Site Energy (kWh) | Saving (%) | Source Energy (kWh) | Saving (%)
M1 | 441951,37 |  | 1439826,96 | 
M2 | 435181,79 | 1.53 | 1411635,35 | 1.96
M3 | 436270,53 | 1.28 | 1415997,94 | 1.65
M4 | 440145,32 | 0.4 | 1431427,23 | 0.58
M5 | 442736,82 | -0.17 | 1441666,33 | -0.13
M6 | 440805,19 | 0.26 | 1434000,91 | 0.41
M7 | 441224,13 | 0.16 | 1435729,03 | 0.28
M8 | 441814,88 | 0.03 | 1438049,840 | 0.12
M9 | 437362,03 | 1.03 | 1420350,17 | 1.35
M10 | 440353,07 | 0.36 | 1432258,39 | 0.53
M11 | 440556,22 | 0.32 | 1433059,8 | 0.47
Only glass sand replacement
Combination of glass sand and glass fiber

## Slide 28
6. Comparison with conventional walls
Table 6.4 Concrete wall layer |  |  |  |  | 
Materials | Thickness (mm) | Thermal conductivity (W/m·K) | Specific heat (J/kg·K) | Density (kg/m3) | Cost
Decorative Plaster | 10 | 0,33 | 2040 | 520 | 1,26 (GBP/m2)
External Panel (M400 Concrete) | 80 | 1,2 | 1000 | 2400 | 21,06 (GBP/m3)
Mineral wool (PAROC WAS 35) | 180 | 0,038 | 840 | 140 | 33,56 (GBP/m3)
Internal Panel (M250 Concrete) | 140 | 0,7 | 1000 | 2400 | 17,55 (GBP/m3)
Gypsum/Cement Plaster | 15 | 0,72 | 840 | 1760 | 0,75 (GBP/m2)
Table 6.5. Comparison between two different wall layer results (annual) |  |  |  | 
Wall Layers | Heating Load (kWh) | Cooling Load (kWh) | Site Energy (kWh) | Source Energy (kWh)
NAAC M2 wall | 338676 | 24206 | 435182 | 1411635
Project Wall | 339422 | 24844 | 435505 | 1413598

## Slide 29
7. Feasibility of NAAC
Civil and Environmental Engineering Department

## Slide 30
7. Feasibility of NAAC
The cost of materials for 1m3 of NAAC
Machinery cost
Electricity cost
Salary for workers
Total 67$ for 1m3 of NAAC
Save from utility bills

## Slide 31
8. CONCLUSION
Civil and Environmental Engineering Department

## Slide 32
8. Conclusion
Successfully develop the mixture proportions
Synergetic effect of combined glass sand and glass fiber on properties of NAAC
Statistical model with high R2 was developed to predict the thermal conductivity of NAAC
Energy saving effect was proved
Recommendations:
The long-term effect of combined glass sand and glass fiber on properties of NAAC
The Alkali – Silica Reaction between the aggregate and cementitious materials
More measurements (more mixture parameters) are needed in order to precisely predict the model based on the Multivariate Linear Regression analysis.

## Slide 33
REFERENCE LIST
References
[1] Jiang, Yi, Tung-Chai Ling, Kim Hung Mo, and Caijun Shi. 2019. "A critical review of waste glass powder–Multiple roles of utilization in cement-based materials and construction products." Journal of environmental management 242: 440-449.
[2] Karazi, S. M., I. U. Ahad, and K. Y. Benyounis. 2017. "Laser Micromachining for Transparent Materials."
[3] Tengri News. 2018. “New life of bottle or how to make money on glass” Received from https://tengrinews.kz/fotoarchive/1048/
[4] Narayanan N, Ramamurthy K. 2000. “Structure and properties of aerated concrete: a review”. Cement, Concrete, Composites Journal 22 (5): 321–29.
[5] Liu, Yiwei, Caijun Shi, Zuhua Zhang, and Ning Li. 2019. "An overview on the reuse of waste glasses in alkali-activated materials." Resources, Conservation and Recycling 144: 297-309.
[6] Liang, Hong, Huiying Zhu, and Ewan A. Byars. 2007. "Use of waste glass as aggregate in concrete." In 7th UK CARE Annual General Meeting. UK Chinese Association of Resources and Environment, Greenwich, vol. 15.
[7] Pehlivanlı, Zühtü Onur, İbrahim Uzun, Zeynep Pınar Yücel, and İlhami Demir. 2016. "The effect of different fiber reinforcement on the thermal and mechanical properties of autoclaved aerated concrete." Construction and Building Materials 112: 325-330.