## Slide 1: Can Geopolymer Concrete become a key Material to utilize Basic Oxygen Furnace Slag (BOFS) as a Construction Material?
Presenter: Gulfairuz Kareken 2nd year Master’s student in Civil & Environmental Engineering
Lead Advisor: Professor Chang-Seon Shon

## Slide 2
Introduction
Problem statement
Possible solution
Research objectives
Experimental program
Test Results
Conclusion
Table of content

## Slide 3
Introduction

## Slide 4: Introduction
gas emission reasons: - Fossil sources
- Disposal of municipal wastes
- Cement production
Alternative material: Green concrete - Geopolymer concrete
aluminosilicate minerals
fine and coarse aggregates
Fly Ash
GGBFS
alkali activators
River sand
BOFS
NaOH

## Slide 5: Introduction
By-product of the steelmaking process:
Basic Oxygen Furnace Slag
Ana P. M. Diniz, Patrick M. Ciarelli, Evandro O. T. Salles, Klaus F. Coco , Heat Transfer in Steel Ladles: Models and Applications DOI: 10.48011/asba.v2i1.1368

## Slide 6: Problem of BOF slags as aggregate
BOFS limits: f-CaO and f-MgO
f-CaO+→ (1)
f-MgO+ (2)
Water expansion
ASR expansion

## Slide 7: Possible solutions
The aluminosilicate (Si-O-Al) framework from geoplymerization process
Si+→ (3)
f-CaO+SiO2 → (4)
f-MgO+SiO2 → (5)
Geopolymer technology and treatment
++2 → + (6)
++2 → + (7)
Lee W.-H., Cheng T.-W., Lin K.-Y., Lin K.-L., Wu C.-C., Tsai C.-T. Geopolymer technologies for stabilization of basic oxygen furnace slags and sustainable application as construction materials, Sustainability, Sustainability 12 (2020) 5002. https://www.mdpi.com/2071-1050/12/12/5002

## Slide 8: Research objectives
Utilize BOFS as an aggregate source and develop an optimum user-friendly mix design
Stabilize BOFS with geopolymerization process without expansion problems
Use carbonation (CO2) curing technique to characterize the expansion behavior of BOFS-based GPC
Provide potential solutions for environmental problems listed in Kazakhstan 2050 strategy: reduction of CO2 emission, the scarcity of land, and the high costs of management and treatment of industrial waste materials

## Slide 9
Experimental Program

## Slide 10: Flow Chart of Experimental Program

## Slide 11: Mixture Design Parameters
Binder content: 60% FA + 40%GGBFS
AAS: 10 M of NaOH and 1, 1.5, and 2 ratios of
Aggregate content: 100% sand
75% sand+25% BOFS
50% sand+50% BOFS
25% sand+75% BOFS
100% BOFS
CO2 curing method for specific samples

## Slide 12: Mix Design
Mixture design parameters
Mixture Group | Mixture No. | Mixture ID | NS (ratio) | BOFS (%) | River Sand (%) | Fly-Ash (kg/m^3) | GGBFS (kg/m^3) | BOFS (kg/m^3) | River Sand (kg/m^3) | NaOH (kg/m^3) | Na2SiO3 (kg/m^3) | Pre-Mix Water (kg/m^3) | Water (kg/m^3) | Total volume (kg/ m^3)
Group 1 | M-1 | 1NS+0%BOFS | 1 | 0 | 100 | 545.01 | 363.34 | - | 605.57 | 51.91 | 181.67 | 129.77 | 106.21 | 1
 | M-2 | 1.5NS+0%BOFS | 1.5 | 0 | 100 | 545.01 | 363.34 | - | 605.57 | 41.52 | 218.01 | 103.81 | 111.58 | 1
 | M-3 | 2NS+0%BOFS | 2 | 0 | 100 | 545.01 | 363.34 | - | 605.57 | 34.6 | 242.23 | 86.51 | 115.03 | 1
Group 2 | M-4 | 1NS+25%BOFS | 1 | 25 | 75 | 548.72 | 365.81 | 152.42 | 457.26 | 52.26 | 182.91 | 130.65 | 110.86 | 1
 | M-5 | 1.5NS+25%BOFS | 1.5 | 25 | 75 | 548.72 | 365.81 | 152.42 | 457.26 | 41.81 | 219.49 | 104.52 | 116.06 | 1
 | M-6 | 2NS+25%BOFS | 2 | 25 | 75 | 548.72 | 365.81 | 152.42 | 457.26 | 34.84 | 243.87 | 87.10 | 119.53 | 1
Group 3 | M-7 | 1NS+50%BOFS | 1 | 50 | 50 | 552.47 | 368.31 | 306.93 | 306.93 | 52.62 | 184.16 | 131.54 | 115.37 | 1
 | M-8 | 1.5NS+50%BOFS | 1.5 | 50 | 50 | 552.47 | 368.31 | 306.93 | 306.93 | 42.09 | 105.23 | 220.99 | 120.61 | 1
 | M-9 | 2NS+50%BOFS | 2 | 50 | 50 | 552.47 | 368.31 | 306.93 | 35.08 | 245.54 | 248.95 | 87.69 | 124.10 | 1
Group 4 | M-10 | 1NS+75%BOFS | 1 | 75 | 25 | 556.24 | 370.83 | 463.53 | 154.51 | 52.98 | 185.41 | 132.44 | 119.94 | 1
 | M-11 | 1.5NS+75%BOFS | 1.5 | 75 | 25 | 556.24 | 370.83 | 463.53 | 154.51 | 42.38 | 222.50 | 105.95 | 125.21 | 1
 | M-12 | 2NS+75%BOFS | 2 | 75 | 25 | 556.24 | 370.83 | 463.53 | 154.51 | 35.32 | 247.22 | 88.29 | 128.73 | 1
Group 5 | M-13 | 1NS+100%BOFS | 1 | 100 | 0 | 560.13 | 373.42 | 622.36 | - | 53.35 | 186.71 | 133.36 | 124.58 | 1
 | M-14 | 1.5NS+100%BOFS | 1.5 | 100 | 0 | 560.13 | 373.42 | 622.33 | - | 42.68 | 224.05 | 106.69 | 129.89 | 1
 | M-15 | 2NS+100%BOFS | 2 | 100 | 0 | 560.13 | 373.42 | 622.33 | - | 35.564 | 248.945 | 88.909 | 133.43 | 1

## Slide 13: Test methods
Test method | Test specification code | Specimen dimension | No. of the test specimen or trial | Testing age (day)
Flowability | ASTM C1437 / C230 | A high of 50 ± 0.5 mm, inside bottom Ø of 100 ± 0.5 mm, and at the bottom, inside top Ø of 70 ± 0.5 mm. | 3 | Immediately after mixing
Air content | ASTM C185 | 400 ± 1 mL | 3 | Immediately after mixing
Setting time | ASTM C191 | A high of 40 ± 1 mm, inside bottom Ø of 70 ± 3 mm, and at the bottom, inside top Ø of 60 ± 3 mm. | 3 | Immediately after mixing
Compressive strength | ASTM C109 | 50 x 50 x 50 mm | 4 | 3, 7, 28, 56 days
Flexural strength | ASTM C348 | 40 x 40 x 160 mm | 4 | 3, 7, 28, 56 days
Drying shrinkage | ASTM C157 | 25 x 25 x 285 mm | 4 | 3- and 4-day intervals (6 months)
Expansion* | ASTM C1260 | 25 x 25 x 285 mm | 4 | 3- and 4-day intervals (28 days)
Dielectric constant | - | 70x70x70 mm | 2 | 3- and 4-day intervals (6 months)
*Note: The expansion test was conducted using the modified ASTM C1260 test method: water and 1M NaOH solution submersion for up to 28 days. |  |  |  | 

## Slide 14: Fresh properties
Test standard: ASTM C1437 / C230
Purpose: determine the flowability of mortar
Test age: Immediately after mixing
Dimension of samples: a height of 50 ± 0.5 mm, bottom Ø of 100 ± 0.5 mm in a cone, and top Ø of 70 ± 0.5 mm in a cone
Relative flowability (Γm) test setup

## Slide 15: Durability test
Test standard: ASTM C1260
Purpose: determination of the aggregate expansion potential for water and the alkali-silica reaction
Dimension of mortar samples: 25x25x285mm
Number samples: 4
Test conditions
  Test solution: water & 1M NaOH solution
  Test age: 3- and 4-day intervals up to 28 days
Chamber at

## Slide 16: Carbonation (CO2) curing of samples
The curing condition:
CO2 concentration: 20%
The relative humidity (RH): 65% ± 5%
The temperature: 23◦C
CO2 curing (exposure) time: 24 hours

## Slide 17
Test Results

## Slide 18: Material Characterization
Material | Specific gravity
FA | 1.9
GGBFS | 2.9
BOFS | 3.1
RS | 2.7
Specific gravity of materials
Particle size distribution of binders

## Slide 19: Material characterization
X-ray Fluorescence of aggregates and binders
Chemical Composition (Wt %) |  |  |  |  |  |  |  |  |  |  | 
 | Na2O | MgO | Al2O3 | SiO2 | SO3 | K2O | CaO | TiO2 | MnO | Fe2O3 | ZnO
FA | 1.03 | 0.53 | 24.85 | 65.34 | 0.31 | 0.68 | 1.86 | 1.10 | 0.07 | 4.01 | 0.04
GGBFS | 1.08 | 12.07 | 12.43 | 35.84 | 2.67 | 0.69 | 33.06 | 1.34 | 0.37 | 0.34 | -
BOFS* | 0.00 | 11.26 | 1.66 | 8.73 | 1.65 | 0.11 | 47.95 | 0.38 | 1.88 | 24.82 | 0.82
RS | 2.97 | 2.29 | 11.83 | 55.85 | 0.67 | 1.88 | 16.13 | 0.77 | 0.85 | 6.53 | -
*Note: free CaO content: 4.47% |  |  |  |  |  |  |  |  |  |  | 
Aggregate Gradation |  |  |  |  |  |  |  |  |  |  | 
 |  | Passing | Retained | Passing | Retained | Passing | Retained | Passing | Retained | Passing | Retained
Sieve size |  | 4.75 mm | 2.36 mm | 2.36 mm | 1.18 mm | 1.18 mm | 600 μm | 600 μm | 300 μm | 300 μm | 150 μm
Mass (%) |  | 10 |  | 25 |  | 25 |  | 25 |  | 15 | 

## Slide 20: Material characterization
X-ray Diffraction of binders (a) and fine aggregates (b)
(a)
(b)

## Slide 21: Material characterization
SEM of BOFS ((a) and (b)) and Fly Ash ((c) and (d))
a) b)
c) d)

## Slide 22: Fresh properties
Flowability of GPM

## Slide 23: Fresh properties
Air content of GPM

## Slide 24: Fresh properties
Setting time of GPM

## Slide 25: Hardened properties
Compressive Strength of BOFS based geopolymer mortar at 3, 7, 28 and 56 days

## Slide 26: Compressive strength test w/ and w/o CO2 curing
Ambient cured GPM
CO2 cured GPM

## Slide 27: Hardened properties
Hardened Density of BOF slag-based geopolymer mortar at 3, 7, 28 and 56 days

## Slide 28: Hardened density w/ and w/o CO2 curing
Ambient cured GPM
CO2 cured GPM

## Slide 29: Hardened properties
Flexural Strength of BOFS based geopolymer mortar at 3, 7, 28 and 56 days

## Slide 30: Flexural strength test w/ and w/o CO2 curing
Ambient cured GPM
CO2 cured GPM

## Slide 31: Hardened properties
Dielectric constant test results of BOF slag-based geopolymer mortar

## Slide 32: Dielectric constant w/ and w/o CO2 curing
Ambient cured GPM
CO2 cured GPM

## Slide 33: Durability properties
Drying shrinkage of BOFS based GPM

## Slide 34: Drying shrinkage w/ and w/o CO2 curing
Ambient cured GPM
CO2 cured GPM

## Slide 35: Durability properties
Water expansion of BOF slag-based geopolymer mortar compared to river sand

## Slide 36: Water expansion w/ and w/o CO2 curing
Ambient cured GPM
CO2 cured GPM

## Slide 37: Durability properties
ASR Expansion of BOF slag-based geopolymer mortar compared to river sand

## Slide 38: ASR expansion w/ and w/o CO2 curing
Ambient cured GPM
CO2 cured GPM

## Slide 39: SEM (after ASR expansion test)
1NS+75% BOFS (ambient cured)
1NS+75% BOFS (CO2 cured)

## Slide 40: Summary of Hardened Properties & Durability

## Slide 41: Response surface methodology
Group A.
25%, 50%, and 75% BOFS-based GPM
Compressive strength = 26.967 - 8.508 Na2SiO3 + 5.377 BOFS - 1.213 (Na2SiO3)2 + 11.882 (BOFS)2 + 0.583 Na2SiO3*BOFS
ASR expansion = 0.03403 - 0.02300 Na2SiO3 + 0.03433 BOFS - 0.0176 (Na2SiO3)2 + 0.0324 (BOFS)2 - 0.02800 Na2SiO3 *BOFS

## Slide 42: Response surface methodology
Group B.
50%, 75%, and 100% BOFS aggregate-based GPM
Compressive strength = 45.046 - 8.937 Na2SiO3 + 3.585 BOFS -1.796 (Na2SiO3)2 - 13.671 (BOFS)2 - 0.820 Na2SiO3*BOFS
ASR expansion = 0.1141 + 0.0052 Na2SiO3 + 0.0495 BOFS - 0.0037 (Na2SiO3)2 -0.0357 (BOFS)2 + 0.0457 Na2SiO3*BOFS

## Slide 43: Conclusion
For compressive and flexural strengths, the GPM mixtures containing BOFS aggregate had comparative strength or higher strength than that containing 100% RS.
Regardless of water and 1M NaOH solution submersions, all GPM mixtures have less than 0.1% expansion value except for the mixture having 75% BOFS and 100 % BOFS aggregate submersed in NaOH solution.
It has been effectively demonstrated that geopolymer technology can stabilize BOFS because GPM mixture’s matrix contains a significant quantity of free silicon (Si), which reacts with free CaO or free MgO to generate stable silicate compounds, solving the problem of BOFS expansion.
CO2 cured samples showed less expansion and less shrinkage than ambient cured samples, but strength performance decreased.

## Slide 44: References
Kuo. W, Gao, Y, C. Juang (2019). Influence of BOF and GGBFS Based Alkali Activated Materials on the Properties of Porous Concrete. “Materials”
W. Lee, T. Cheng, K. Lin, K. Lin, C. Wu, C. Tsai (2020) Geopolymer Technologies for Stabilization of Basic Oxygen Furnace Slags and Sustainable Application as Construction Materials. Sustainability
M. Mastali, A. Alzaza, K. Shaad, P. Kinnunen, Z. Abdollahnejad, Bethany Woof, M. Illikainen (2019). Using Carbonated BOF Slag Aggregates in Alkali-Activated Concretes. “Materials”
A. Krishna Rao, D. Rupesh Kumar (2020). Comparative study on the behaviour of GPC using silica fume and fly ash with GGBS exposed to elevated temperature and ambient curing conditions. “Materials Today: Proceedings”
P. Azarsaa , R. Gupta (2020). Durability and leach-ability evaluation of K-based geopolymer concrete in real environmental conditions. “Case Studies in Construction Material”
M. Ma, H. Mehdizadeh, M. Guo, T. Ling (2021). Effect of direct carbonation routes of basic oxygen furnace slag (BOFS) on strength and hydration of blended cement paste. “Construction and Building Materials” A. Karthik, K. Sudalaimani, C.T. Vijaya Kumar (2017). Investigation on mechanical properties of fly ash-ground granulated blast furnace slag based self curing bio-geopolymer concrete. “Construction and Building Materials”
L. Yunxia, Z. Mingkai, C. Xia, X. Fang(2008). Methods for Improving Volume Stability of Steel Slag as Fine Aggregate. “Journal of Wuhan University of Technology-Mater”
Y. Ding, T. Cheng, P. Liu, W. Lee (2017). Study on the treatment of BOF slag to replace fine aggregate in concrete. “Construction and Building Materials”
M.S.H. Khan, A. Castel, A. Noushini. CARBONATION OF A LOW CALCIUM FLY ASH GEOPOLYMER CONCRETE. “Centre for Infrastructure Engineering and Safety, School of Civil and Environmental Engineering, The University of New South Wales, Sydney, NSW 2052, Australia.”
W. Kuo, C. Shu (2013). Application of high-temperature rapid catalytic technology to forecast the volumetric stability behavior of containing steel slag mixtures. “Construction and Building Materials”
N. Kabay, N. Miyan, H. Ozkan (2021). Basic oxygen furnace and ground granulated blast furnace slag based alkali-activated pastes: Characterization and optimization. “Journal of Cleaner Production

## Slide 45: Thank you for your attention!