## Slide 1: Fabrication of metal powder for additive manufacturing using ultrasonic atomizer Isaac Iwediba 2nd Year Master in Mechanical and Aerospace Engineering Supervisor: Prof. Didier Talamona Co-Supervisor: Prof. Asma Perveen

## Slide 2: Outline
Introduction
Research Objectives
Literature review
Method
Results
Conclusion/Future work

## Slide 3: Overview
Step 1
Step 2
Step 3
Review literature
&
research gap
Identification
Application of
ultrasonic atomization
technique
Characterization of fabricated and commercial powders
SLM 3D
Printing &
mechanical testing
Step 4
Results, conclusion & Future work
Step 5

## Slide 4: Introduction (1)
Reduction of metals to powder form e.g Al, Fe, Mg,W, Mo, Ni, Ti and Cu etc.
Base material for the production of metallic components through
additive manufacturing, Powder Metallurgy, Casting, etc.
Flexibility, reduced waste, speed, customization, cost effective.

## Slide 5: Introduction (2)
.
Metal powder market research [2]
Report highlights | Details
Market size | USD 8.52 Billion by 2027
Growth rate | CAGR 6.19% from 2020 -2027
Largest market | North America
Fastest growing market | Asia Pacific

## Slide 6: Applications of metal powder
Fabrication techniques
Powder metallurgy
Additive manufacturing
surface coating
chemical reactions(reducing agents), etc.

## Slide 7: Research objectives
Investigation & Optimization
Benchmark
Mechanical Testing
Printability
Investigate & optimize the ultrasonic atomization process for stainless steel 316L.
To investigate the printability characteristics of the fabricated powder.
To benchmark the commercially produced Stainless steel 316L powder with the ultrasonic fabricated Stainless steel 316L.
To test the printed part for hardness and tensile strength

## Slide 8: Literature review (1)
Production process | Material | Range of particle size µm | Advantages | Disadvantages | references
Rotating electrode plasma process | Tungsten wire | 160-500 | More spherical, ultra-clean particles. | Inefficient production at high cost, Broad particle size range | [16, 17]
Gas atomization | Ti Alloy | 0-250 | More spherical shape, Used for a variety of alloy metals with reactive qualities that are available as ingots, spherical particles. | Broad particle size range. | [18]
Plasma atomization | Ti Alloy | 25 - 125 | Presence of spherical particles | Expensive wire or powder-based feedstock is required. | [19]
Water atomization | AlSi316L | 44-106 | Large range of particle sizes, high manufacturing speeds, ingredients in ingot form. | Wide distribution of particle sizes and irregularly shaped particles are all removed by a separate procedure. | [20]
Centrifugal atomization of plasma | HSS, Ti Alloy, 45 steel | 0-385 | Round particles that are easily manufactured | The distribution of particle size’s fractional content is highly diverse. | [21]
Centrifugal Atomization | Magnesium Alloy | 50-800 | There is a wide variety of particles sizes, although the distribution is restricted. | Creating high-quality powder is difficult. Higher particle size | [22]

## Slide 9: Research Gap
WHY?
Inconsistent Size, Shape, and Surface characteristics
Costly to produce: especially when high-purity powders are needed for specialized applications.
Flowability

## Slide 10: Scope & constraints
Constraints
Scope
High consumption rate of Argon
Low production rate
Powder fabrication
Powder benchmark
Mechanical Testing
Powder Characterization
SLM 3D Printing

## Slide 11: Methodology (1)
Powder fabrication
Optimization process parameters
Amplitude
Current
Feed rate
Characterization measurements:
Particle size distribution ‘PSD’ (mastersizer)
Rheological properties/test (FT4 Powder Rheometer)
Stability and variable flow
  Permeability
  Shear cell
  Aeration
  Compressibility
Flow rate(Hall Flowmeter)
Angle of repose (Hall Flowmeter)
Printability of the produced powder (SLM)
Mechanical Testing
Tensile
Hardness
(SEM) Analysis
Particle shape
Particle size
chemical composition

## Slide 12: Methodology (2)

## Slide 13: Atomizer process condition
Experiment Number | Electrical current, A | Ultrasonic vibration amplitude, % | Main circuit pump flow, % | Argon flow, l/min | Feeder speed (%) | Voltage (V)
1 | 110 | 70 | 65 | 10 | 25 | 22.20
2 | 120 | 75 |  | 15 | 45 | 
3 | 130 | 80 |  | 20 | 50 | 
Orthogonal Arrays (Taguchi Designs) for the fabrication of steel 316L (Wire Ø 1.2mm)

## Slide 14: Fabrication rate
Exp. no | Time (hr) | Consumption of Argon (bar) | Amount of Powder in powder container (g) | Amount of sieved powder(g) 63µm | Amount of sieved powder(g) 100µm | Productivity Sieved Powder 63 µm (g/hr) | Amount of un-sieved powder(g/hr)
1 | 19 | 320 | 1458 | 1000 | 134 | 53 | 77
2 | 24 | 700 | 2086 | 1400 | 260 | 58 | 87
3 | 5 | 150 | 1100 | 800 | 110 | 160 | 220
Total | 48 | 1170 | 4644 | 3200 | 505 |  | 
Fabrication of Stainless steel 316L at 0°

## Slide 15: Effect of Current and Amplitude
 | Current (A) | Time | Constant Parameter | Manipulator Position |  | 
 |  |  |  | X | Y | Z
Effect of Current | 120 | 1hr | 120 A | 10.00 | 16.00 | 9.50
 | 130 | 1hr |  |  |  | 
Effect of Amplitude | 75% | 1hr | 80% |  |  | 
 | 80% | 1hr |  |  |  | 
Ultrasonic Atomization Fabrication Optimum parameters |  |  |  |  | 
Electrical current, A | Ultrasonic vibration amplitude, % | Main circuit pump flow, % | Argon flow, l/min | Feeder speed (%) | Voltage (V)
130 | 80 | 65 | 20 | 50 | 22.50

## Slide 16: Characterization techniques
SEM
Hall Flow meter
Master sizer
FT4 Powder Rheometer

## Slide 17: SEM Images
SEM images
(a) and (b) commercially produced stainless steel powder at a scale of 50 and 100µm
(c) and (d) ultrasonic fabricated stainless steel powder at a scale of 50 and 100µm

## Slide 18: Chemical Compositions
Element | Mass% | Atom%
Si | 0.50±0.04 | 1.00±0.09
Cr | 19.43±0.17 | 20.81±0.18
Mn | 2.58±0.09 | 2.62±0.09
Fe | 63.21±0.35 | 63.05±0.35
Ni | 11.47±0.19 | 10.89±0.18
Mo | 2.81±0.11 | 1.63±0.06
Total | 100.00 | 100.00
Element | Mass% | Atom%
Si | 0.58±0.04 | 1.15±0.07
Cr | 18.37±0.15 | 19.67±0.16
Mn | 2.03±0.07 | 2.06±0.08
Fe | 64.55±0.32 | 64.35±0.31
Ni | 11.89±0.18 | 11.27±0.17
Mo | 2.58±0.09 | 1.50±0.05
Total | 100.00 | 100.00
Atomized SS 316L
Commercial SS 316L

## Slide 19: Average Particle Diameters
Powder sample | no of particles | Average particle diameters (µm) | Average areas (µm²)
Commer- cial steel | A 84 D 161 | 29.36 | 730.37
Ultrasonic fabricated steel | A 66 D 133 | 43.82 | 1609.28
Average particles diameters and areas of Stainless Steel 316L
& (b) diameter and area of commercial Stainless steel powder
(c) & (d) diameter and area of ultrasonic fabricated Stainless steel powder.
²
²
²
²

## Slide 20: Rheological properties
Test name | Commercial Stainless steel powder 316L | Ultrasonic fabricated Stainless steel 316L
Conditioned bulk density (g/cm3) | 4.77 | 4.73
Compressibility index (%) | 2.85 | 3.00
Pressure drop (mBar) | 5.87 | 3.26
Specific energy (mJ/g) | 2.43 | 2.35
Aeration energy (mJ) | 11.49 | 12.47
Basic flow energy (mJ) | 845.69 | 828.4
Cohesion coefficient (kPa) | 0.36 | 0.23

## Slide 21: Rheological properties
The Rheological properties was used to calculate the Additive Manufacturing suitability (AMS) factor of the powders[5,38].
The smaller the AMS values, the more suitable the powder is for the additive manufacturing process.
Powder Sample | AMS Factor
Ultrasonic fabricated SS 316L | 0.87
Commercial SS 316L | 0.98

## Slide 22: AOR & Flowrates
AOR | Properties of flow
20° < Φ <30° | Very unconstrained
30° < Φ <39° | unconstrained
39° < Φ <44° | Acceptable to fair flow
44° < Φ <54° | adhesive
554° <Φ <69° | Very adhesive
The AOR classification of flow characteristics[81]
Powder sample | Commercial Stainless steel powder 316L | Ultrasonic fabricated Stainless steel 316L
AOR (degree) | 28.1 ± 0.2 | 24.6 ± 0.1
Flowrate (minutes) | 1.22 ± 0.1 | 1.14 ± 0.1
AOR and Flowrate readings for the sample powders

## Slide 23: Particle size distribution

## Slide 24: Physical characteristics
Sample powder | Tap density (g/cm³) | 𝑃𝚙,а (g/cm³) | 𝑃𝚙,а(g/cm³) literature | Hausner ratio | Carr’s index | Porosity
Commercial SS 316L | 4.92 | 7.0 | 8.0 [9] | 1.10 | 9.20 | 0.33
Ultrasonic fabricated SS 316L | 5.0 | 8.0 | 8.0 [9] | 1.11 | 10.0 | 0.44

## Slide 25: SLM 3D Printing
Standard Tensile Samples
AM 400 Renishaw view

## Slide 26: Tensile Test
Tensile Test for the standard tensile sample

## Slide 27: Vickers Hardness Test
Exp no. | Vickers | Load | Dwelling time (sec)
1 | 200.99 HV/1 | 9.8N | 10
2 | 201.87 HV/1 | 9.8N | 10
3 | 204.07 HV/1 | 9.8N | 10
4 | 207.32 HV/1 | 9.8N | 10
5 | 198.98 HV/1 | 9.8N | 10

## Slide 28: Mechanical Properties
Grade | SS 316L | SS 316L Literature [93]
Yield strength, MPa | 464 | 519.0
Tensile strength, MPa | 597 | 633
Ductility | 6.6 | 
%Elongation after fracture | 48 | 32.45
Young’s modulus, GPa | 235.7 | 207.2
Hardness maximum | 207.32 HV/1 | 247 HV [94]

## Slide 29: Conclusion
Fabrication Optimum parameter
Current of 130A, amplitude of 80%, and feeder speed rate of 50%.
Printing
High-quality metal components with superior mechanical qualities as observed in the printed standard tensile sample.
Benchmark
Commercially available powder is a lower grade powder
Both powders have rheological characteristics that are advantageous for additive manufacturing methods.
Mechanical Testing
Tensile and hardness tests on the printed standard samples revealed that its mechanical characteristics fell within the allowed range.
Higher young’s modulus of elasticity indicates that the SS 316L is suitable for load bearing structures.

## Slide 30: Future work
Further study of stainless steel 316L fabrication using ultrasonic atomizer is required to enhance its mechanical and corrosion resistant qualities given the rising demand for high-performance materials across a variety of industrial sectors.
Exploring the usage of different manipulator angles
The fabricated powder should also be analyzed to make sure it has a nearly perfect spherical shape
Printing of the powder can be carried out to further test the final product’s mechanical qualities.

## Slide 31: References
[1] V. N. Korzhyk et al., "New Equipment for Production of Super Hard Spherical Tungsten Carbide and other High-Melting Compounds Using the Method of Plasma Atomization of Rotating Billet," Materials Science Forum, vol. 898, pp. 1485-1497, 06/01 2017, doi: 10.4028/www.scientific.net/MSF.898.1485.
[2] https://www.precedenceresearch.com/metal-powder-market (accessed 15 April 2023).
[3] https://www.beamler.com/3d-printing-capabilities/processes/slm-selective-laser-melting/ (accessed 15th April, 2023).
[4] A. Alagheband and C. Brown, "Plasma Atomization goes commercial," Metal Powder Report, vol. 53, pp. 26-28, 11/01 1998, doi: 10.1016/S0026-0657(99)80007-1.
[5] S. E. Brika, M. Letenneur, C. A. Dion, and V. Brailovski, "Influence of particle morphology and size distribution on the powder flowability and laser powder bed fusion manufacturability of Ti-6Al-4V alloy," Additive Manufacturing, vol. 31, p. 100929, 2020/01/01/ 2020, doi: https://doi.org/10.1016/j.addma.2019.100929.
[6] S. Bogdanov, "Prospects of Production of Granular Composite Materials by Method of the Plasma-Centrifugal Atomization," Metallurgist, vol. 61, 04/13 2018, doi: 10.1007/s11015-018-0615-0.
[7] C. Labrecque, R. Angers, R. Tremblay, and D. Dub, "Inverted Disk Centrifugal Atomization of AZ91 Magnesium Alloy," Canadian Metallurgical Quarterly, vol. 36, pp. 169-175, 07/01 1997, doi: 10.1016/S0008-4433(97)00007-4.
[8] W. Gao et al., "The status, challenges, and future of additive manufacturing in engineering," Computer-Aided Design, vol. 69, pp. 65-89, 2015/12/01/ 2015, doi: https://doi.org/10.1016/j.cad.2015.04.001.
[9] G. Çakmak, M. B. Donmez, A. R. Cuellar, Ç. Kahveci, M. Schimmel, and B. Yilmaz, "Additive or subtractive manufacturing of crown patterns used for pressing or casting: A trueness analysis," Journal of Dentistry, vol. 124, p. 104221, 2022/09/01/ 2022, doi: https://doi.org/10.1016/j.jdent.2022.104221.
[10] M. Lalegani Dezaki et al., "A review on additive/subtractive hybrid manufacturing of directed energy deposition (DED) process," Advanced Powder Materials, vol. 1, no. 4, p. 100054, 2022/10/01/ 2022, doi: https://doi.org/10.1016/j.apmate.2022.100054.
[11] M. Akbari and N. Ha, "Impact of additive manufacturing on the Vietnamese transportation industry: An exploratory study," The Asian Journal of Shipping and Logistics, vol. 36, no. 2, pp. 78-88, 2020/06/01/ 2020, doi: https://doi.org/10.1016/j.ajsl.2019.11.001.
[12] S. Junk and N. Rothe, "Lightweight design of automotive components using generative design with fiber-reinforced additive manufacturing," Procedia CIRP, vol. 109, pp. 119-124, 2022/01/01/ 2022, doi: https://doi.org/10.1016/j.procir.2022.05.224.
[13] V. Madhavadas et al., "A review on metal additive manufacturing for intricately shaped aerospace components," CIRP Journal of Manufacturing Science and Technology, vol. 39, pp. 18-36, 2022/11/01/ 2022, doi: https://doi.org/10.1016/j.cirpj.2022.07.005.
37. Source: https://www.polarismarketresearch.com/industry-analysis/metal-powder-market
[38] https://3dprintingindustry.com/news/new-research-proposes-am-suitability-factor-for-metal-powder-selection-202992/ (accessed 16th April, 2023)

## Slide 32: Thank you for your attention!