## Slide 1
BATTERY STATE OF HEALTH DETERMINATION THROUGH VARIOUS TECHNIQUES
Lead supervisor: Prof. Zhumabay Bakenov
Co-supervisor: Dr. Berik Uzakbaiuly

## Slide 2: Outline
Goal and importance
Flow process work chart
Experimental part
Results and Discussion
  LiSOCl2 -entropy
  NCR - entropy
  NCR AI technique
2

## Slide 3: Goal and Importance
- Lithium ion batteries problems
  Longevity
  Safety
Current technology:
Machine learning(AI), Electrochemical model,
Mathematical model, EIS
2. Goal
  Non-invasive
  Quick
  Precise
  Entropymetry and ML
3

## Slide 4: SOH
SOH = Q/Q(init)
Q - actual maximum capacity
Q(init) - initial maximum capacity
4
SOC
SOC = Qrem/Q(full)
Qrem – remaining capacity
Q(full) – full charged capacity

## Slide 5
Experimental part
5

## Slide 6: Basic equations
Equations for thermodynamics parameter calculation
6
E - open circuit voltage of the battery
F – Faraday’s constant
T – temperature
n – number of electrons

## Slide 7: Mathematical model of SOC estimation
SOH = f(α, β, γ)
Mathematical model of SOH estimation
7

## Slide 8: Thermal chamber
8

## Slide 9: Methodology of entropy calculation at various SOC (slow method)
1 . Determining the discharge capacity of the battery at 0,05 C-rate
2. Full charging of the battery at 0.05C and set as 100% state of charge
3. And discharging to appropriate SOC, waiting for equilibrium (12 h)
4. Determining the voltage of battery at various temperatures (0 - 30) and SOC.
9

## Slide 10: Methodology for new approach (fast method)
1 . Determining the discharge capacity of the battery at 0,05 C
2. Full charging of the battery at CCCV mode
And discharging of battery for 11 % SOC change
Charging of battery for 1 % SOC change
5. Waiting for equilibrium (20 min)
6. Determining the voltage of battery after eq. at various temperatures
Previous method: 18 h / (10% SOC step)
New method: 4,5 h/ (10% SOC step)
10

## Slide 11
Results
LiSOCl2 Primary battery
Nominal voltage 3,5 V
Capacity 1000 mah
11

## Slide 12: Charge discharge profile of LiSOCl2 battery at various C-rate.
12

## Slide 13
Entropy profile of the lithium thionyl battery at various SOC.
13

## Slide 14
14
SOH estimation model for lithium thionyl battery

## Slide 15: Results
NCR battery
Nominal voltage 3,7 V
Capacity 3200 mah
15

## Slide 16
Sample1 – NCR18650
16

## Slide 17
Sample1 – NCR18650
17

## Slide 18
G, H, S vs SOC of Sample1 – NCR18650
18

## Slide 19
Entropy measurement with various approach
19

## Slide 20
Entropy profile of NCR18650 parameters at various cycle numbers
20

## Slide 21
α | β | γ | R^2
- 371,2985 | 0,4789 | -1,1788 | 0,99428
NCR18650
21

## Slide 22
22
Linear regression coefficients at various state of health of the battery
SOH = f(α, β, γ)

## Slide 23
Artificial Intelligence
Results
23

## Slide 24
24

## Slide 25
Charge discharge profile of NCR 18650 at 1,5 C
25

## Slide 26
26

## Slide 27: . The precision of each machine learning algorithm
27
- The model can be applied at the following condition: 1,5 C rate, T = 25 C, DOD = 100%
- Need more data to apply for other conditions

## Slide 28: Conclusion
28
Mathematical model in which entropy depends on state of charge of the battery by 6th order polynomial function was suggested, showed R2 higher than 0.95 (LiSOCl2)
New Entropy measurement technique is developed
The change of entropy profile at various state of health was indicated
The machine learning method was proposed for SOH estimation of NCR18650 battery
LSTM technique has high accuracy of the estimation among algorithms

## Slide 29
Thanks